## Slide 1
Phase transformation and precipitation kinetics in V-micro-alloyed steels
Project: Resource efficient NANO-steels through in-situ and simultaneous studies of the precipitation and phase transformation kinetics
Project number : S41.5.14548a
C. Ioannidou, A. Navarro, Z. Arechabaleta, X. Zhang, A. Rijkenberg, R. M. Dalgliesh, S. Kölling,
V. Bliznuk, B. Kooi, C. Pappas, J. Sietsma, A. A. van Well, S. E. Offerman
TUDelft
Project leader: S.E.Offerman
Daily supervisors: S.E.Offerman, A.A. van Well
Industrial partners
TATA Steel, M2i, VDL, Nedschroef

## Slide 2
1. Improve fuel economy and resource efficiency through vehicle weight reduction
2. Achieve high strength, ductility and flange-ability in chassis and suspension parts
Conventional AHSS cannot provide this beneficial combination of properties
Challenges for Automotive Industry

## Slide 3
strength
ductility
Nano-Steels
single-phase ferrite structure with nano-precipitates
Vanadium
best suited for strong precipitation strengthening
save alloying costs
Study the precipitation & phase transformation kinetics in V-micro-alloyed steels
Scientific Aim
50nm
neutrons
Challenges for Automotive Industry
Research Approach

## Slide 4
Outline, ex-situ
Acta Materialia 181 (2019) 10–24
Heat treatment
Precipitation & phase transformation kinetics
in V-micro-alloyed steels

## Slide 5
Chemical composition (wt.%), balance Fe
Steel | C | Mn | V
LCLV | 0.071 | 1.84 | 0.29
HCHV | 0.135 | 1.83 | 0.57
10x10x1mm3
dilatometer
higher C content in HCHV, which stabilizes the austenite and delays the onset of phase transformation
V can retard ferrite nucleation due to segregation at austenite grain boundaries
Phase transf & precip detected only at 650oC
Alloys, heat treatments & phase transformation kinetics

## Slide 6
In dilatometry treated samples
beam size 5x5mm2
0.41<λ<1.33nm
sample thickness 1mm
ex-situ
SANS - Precipitation kinetics
LARMOR

## Slide 7
2D pattern
1D
SANS - Precipitation kinetics

## Slide 8
TEM, spherical ellipsoidal precipitates
Interphase precipitation
Interphase/Random precipitation
SANS - Precipitation kinetics

## Slide 9
More precipitates in the HCHV steel
SANS - Precipitation kinetics

## Slide 10
Nucleation + growth
dominant
Growth + Coarsening
dominant
SANS - Precipitation kinetics

## Slide 11
Precipitate size distribution
Peak increases
nucleation
Peak to the right
Larger precipitates
Peak broadening
growth/coarsening
SANS - Precipitation kinetics

## Slide 12
Precipitation during (area 1) and after the phase transformation (area 2).
Area 1: precipitates in rows (interphase precipitation)
Area 2: randomly dispersed precipitates
Phase transformation & Precipitation kinetics

## Slide 13
V maps
Size distribution
Same samples treated in dilatometry and tested by SANS
Atom Probe Tomography - Precipitation

## Slide 14
APT values for
Rm, Np, fV
Consistent to SANS
Volume analyzed by
APT~ 106 nm3
SANS 1020 nm3
Atom Probe Tomography - Precipitation

## Slide 15
Precipitate chemical composition evolution
Atom Probe Tomography - Precipitation

## Slide 16
At 650oC interphase precipitation of VC takes place (not at 750 and 900oC)
Nucleation and growth are dominant during the first 20 min, while later precipitate growth with soft impingement (overlapping diffusion fields) and coarsening take place.
The steel with two times higher vanadium and carbon concentrations (HCHV) exhibits x2 higher volume fraction and number density of the precipitates after 10 h of annealing.
The precipitate chemical composition evolution during annealing is strongly correlated to their size.
Summary

## Slide 17
Neutron
Beam
ND
SANS
LARMOR
rotation 20o
40o/min
beam size 8x8mm2
sample thickness 1mm
1min time resolution
In-situ simultaneous SANS & Neutron Diffraction
Real time measurements
Phase transformation & precipitation kinetics simultaneously
same sample volume, avoid effects of inhomogeneities
Improved background subtraction for SANS compared to ex-situ measurements
Precipitate chemical composition evolution
Adapt heat-treatments based on real time obtained results

## Slide 18
precipitation follows phase transformation (high solubility of VC in austenite, then interphase precipitation)
precipitation during (interphase precipitation) and after the phase transformation
phase transformation
& precipitation
precipitation
by ND
by SANS
Phase transformation & precipitation kinetics

## Slide 19: Industrial aim of the project
Results provide
quantitative information focused on the kinetics of the VC in low-carbon steels,
quantitative information on precipitation interaction with austenite-to-ferrite phase transformation,
quantitative information on the evolution of the precipitate chemical composition,
role of micro-alloying elements on the phase transformation and precipitation kinetics
Use of the quantitative results
as input parameters for modeling the precipitation kinetics in V micro-alloyed steels, which may lead to improved steel design and performance for automotive applications.

## Slide 20: Thank you