## Slide 1: Reconnecting the values of carbon and steel: In the carbon lean prospect
M2I Conference/ Noordwijkerhout, the Netherlands/ 10-12-19
Güçhan Yapar

## Slide 2: Tata Steel Site, IJmuiden
2
Raw materials to hot metal
2

## Slide 3: Iron and steel making: current practice
1. Raw materials
2. Blast furnace
3. Steel shop
and casters
4. Down-stream
Strip steel
Coal
Blast furnace gas
Basic oxygen furnace gas
Limestone
Natural gas
Gas Network
1 t
0.5 t
0.1 t
0.03 t
1.4 GJ
Hot metal
Steel cast
Coke, PC
BF gas dust
Coke fines
Steel scrap
Coke oven gas
Combustion
Thermal energy
Electricity
CO2
CO2
Tar, benzole: Export streams
Carbon is the main reactant in the Blast furnace iron-making process.
Residual energy in the steel mill off - gases is released with combustion.

## Slide 4: CO2 emission performance: Tata Steel Europe
World Steel Benchmark performance1
WAG blends are combusted to facilitate heat exchange:
I&S works
Power plants
Site IJmuijden specific emissions: 1.7 t CO2eq./ t CrudeSteel
Site energy integration reduces energy import and CO2 emissions on site.
Further reduction in the CO2 footprint of steel is necessary to reach 2030 goals !

## Slide 5: Gas network: Re-thinking
Contain the gaseous carbon in transport ready for storage and utilisation form
Feedstock to CCS/U is rich in CO and CO2; i.e. CO is the main chemical energy carrier
Power supply from de-carbonized grid: higher penetration of wind and solar based power
Natural gas import to recover energy deficit in the I&S works and CCS/U plant
Works Arising Gases (WAGs) as feedstock for CCS/U
BFG: Blast furnace Gas
BOFG: Basic oxygen furnace gas
COG: Coke oven gas
NG: Natural Gas
Heat and power generation

## Slide 6: Gas network: Re-thinking
Contain the gaseous carbon in transport ready for storage and utilisation form
Feedstock to CCS/U is rich in CO and CO2; i.e. CO is the main chemical energy carrier
Power supply from de-carbonized grid: higher penetration of wind and solar based power
Natural gas import to recover energy deficit in the I&S works and CCS/U plant
Works Arising Gases (WAGs) as feedstock for CCS/U
BFG: Blast furnace Gas
BOFG: Basic oxygen furnace gas
COG: Coke oven gas
NG: Natural Gas
Heat and power generation

## Slide 7: CCS/U concept: Re-use carbon feedstock and store un-used CO2
Methanol (Hydrogenation) :
Alkane and alkene chains
(F-T synthesiz) :
Thermo – chemical conversion to re-use as transport fuel and/ or base materials
Current steel mill gas scheme does not readily supply H2 to convert all carbon;
H2 : (CO+CO2) = 1 : 10 mols.
CCS/U application requires gas processing and compression steps up-stream to the chemical plants.

## Slide 8: Gas processing and compression: Upgrade to syngas
Water electrolysis:
50 kWhel/ kg H2 (large scale Alkaline)
Produces O2 as side product
Post-compression
H2 enrichment
Water – gas shift:
Feed condition of HTS*: 18 bar, 623 K
Gas is enriched in CO2 and H2
Reaction generates entalphy (20.5 MJ/ kg H2)
Selective Process: CO2 capture from BFG with alkanol-amines; e.g. MeA
CO2 reclaim with steam re-boiler
* HTS: High temperature shift
CO2 capture
Chemical absorption (State of art)
(Electro-chemical)
(Thermo-chemical)

## Slide 9: CCU in the Perspective to the Steel Industry

## Slide 10: HIsarna: Alternative iron making process for CCS/U
Oxygen is injected for an oxi-combustion of the rising gas
Avoided N2 enables energy consumption reduction in the CCS plant
Top gas is concentrated with CO2 at 1600 °C; i.e. almost full oxidation
CO2 reduction up to 50 % by scrap and biomass injection (without CCS)
Tata Steel IJmuiden
Future developments of Hisarna:
Continual development of technology at Hisarna Pilot Plant
Demo plant in Tata Steel, Jamshedpur
Demo plant with CO2 capture and storage at Tata Steel, NL (1Mtpa)

## Slide 11
From Residual Steel Mill Gases to Methanol

## Slide 12: End of pipe application: FReSMe project (H2020)
BFG upgrading facility from “Stepwise” and Methanol synthesis equipment from “MefCO2” projects (H2020) are combined.
Carbon capture rate > 95 %mol
N2 content in CO2 – rich
stream < 1 %mol
H2/ N2 separation by membranes
Additional H2 production by electrolysis
CO2 based MeOH synthesis
FReSMe will demonstrate the production of Methanol (MeOH) using as feedstock CO2 from Blast Furnace Gas (BFG) at TRL6

## Slide 13: CO2 capture in MeOH with FReSMe: In the carbon lean prospect
Carbon yield in MeOH increases with external H2
De-carbonized grid favors MeOH production with green H2 supply (electrolysis)
40 - 45 %mass CO2 reduction* by FReSMe with fully de-carbonized electricity
*Reference European steel mill and natural gas based MeOH plant (without CO2 capture)
H2 available from SEWGS convert 10 %mass CO2 to MeOH
Excess CO2 is ready for storage after compression step
CO2 storage is required with current European grid emissions
STEPWISE
MefCO2

## Slide 14: Final Remarks:
In the current practice, steel mill WAG’ s supply electricity and thermal energy internally and leave the system as CO2 emissions
CCS/U is an end of pipe approach to re-use the carbon feedstock in the steel mill gases and store un-used CO2
HIsarna is a breakthrough iron-making technology to reduce CO2 and produce capture ready top gas
FReSMe captures carbon in the steel mill gases in MeOH by making use of green Hydrogen
Smart combination of carbon storage and utilisation is necessary to achieve 2030 goals
Industrial level FReSMe should be flexible with dynamic solar and wind powered electricity grid

## Slide 15
On our way to CO2-neutral steelmaking in 2050

## Slide 16: Do you have any questions?
        Tata Steel
Research and Development
Guchan.Yapar@tatasteeleurope.com
www.tatasteeleurope.com